### **GIA REPORT NUMBER**16383275 **DATE OF ISSUE** Nov. 6, 2007

# COLORED DIAMOND GRADING REPORT

**FOR NATURAL DIAMOND**

**CUT-CORNERED RECTANGULAR MODIFIED BRILLIANT**

|  |  |
| --- | --- |
| Measurements | **14.28 x 13.47 x 9.06 mm** |
| Carat Weight | **16.92 carat** |
| Clarity Grade | **VS1** |

**COLOR**

|  |  |
| --- | --- |
| Origin | **Natural** |
| Grade | **Fancy Yellow** |
| Distribution | **Even** |

**PROPORTIONS**

|  |  |
| --- | --- |
| Depth | **67.3** **%** |
| Table | **72** **%** |
| Girdle | **Very Thick to Extremely Thick** |
| Culet | **None** |
|  |  |

**FINISH**

|  |  |
| --- | --- |
| Polish | **Excellent** |
| Symmetry | **Very Good** |

**FLUORESCENCE**

|  |  |
| --- | --- |
| Fluorescence | **None** |

**CLARITY CHARACTERISTICS**

|  |  |
| --- | --- |
| Clarity Characteristics | **Feather, Pinpoint, Natural, Extra Facet** |