**GIA REPORT NUMBER** 16383269 **DATE OF ISSUE** Nov. 13, 2007

COLORED DIAMOND GRADING REPORT

**FOR NATURAL DIAMOND**

**CUT-CORNERED SQUARE MODIFIED BRILLIANT**

|  |  |
| --- | --- |
| Measurements | **14.22 x 13.54 x 8.93 mm** |
| Carat Weight | **16.36 carat** |
| Clarity Grade | **VS1** |

**COLOR**

|  |  |
| --- | --- |
| Origin | **Natural** |
| Grade | **Fancy Yellow** |
| Distribution | **Even** |

**PROPORTIONS**

|  |  |
| --- | --- |
| Depth | **66.0** **%** |
| Table | **71** **%** |
| Girdle | **Very Thick** |
| Culet | **None** |
|  |  |

**FINISH**

|  |  |
| --- | --- |
| Polish | **Excellent** |
| Symmetry | **Excellent** |

**FLUORESCENCE**

|  |  |
| --- | --- |
| Fluorescence | **None** |

**CLARITY CHARACTERISTICS**

|  |  |
| --- | --- |
| Clarity Characteristics | **Cloud, Needle, Extra Facet** |
|  |  |

**COMMENTS**

Surface graining is not shown.